TEST NAME – Thermal Test

(As per IEC 62660-2)

1. Purpose

The Thermal Abuse Test is conducted to evaluate the safety behaviour and Characterize cell responses of a lithium-ion battery cell when exposed to extreme Temperature conditions.

This test is intended to:

- Assess thermal stability of the cell at high temperatures

- Identify risks of venting, fire, explosion, or thermal runaway

- Evaluate robustness of internal cell materials and safety features

- Demonstrate compliance with IEC 62660-2 thermal abuse requirements

2. Scope

This procedure applies to:

- Secondary lithium-ion cells for propulsion applications

- Pouch, cylindrical, and prismatic cell formats

- Cell-level safety and abuse qualification testing

This test is performed in accordance with:
IEC 62660-2: Secondary lithium-ion cells for propulsion of electric road vehicles – Part 2: Reliability and abuse testing

3. References

- IEC 62660-2 – Reliability and abuse testing

- Cell manufacturer datasheet

- Internal battery abuse and safety procedures

4. Equipment & Tools

- Temperature-controlled thermal chamber or oven

- Calibrated thermocouples or temperature sensors

- Voltage monitoring system

- Fire-rated abuse test chamber (if oven is not fireproof)

- Fire suppression and exhaust system

- Data acquisition system

5. Safety Precautions

- Perform the test only in a fire-rated thermal abuse chamber

- Wear full PPE: safety goggles, heat-resistant gloves, flame-retardant clothing

- Ensure fire suppression and emergency shutdown systems are active

- Do not open the chamber during heating or soak phase

- Abort the test only if chamber integrity or safety systems are compromised

6. Test Setup

6.1 Mechanical Setup

- Place the cell on a non-combustible, thermally stable holder

- Ensure the cell is not mechanically constrained

- Allow free venting of gases

6.2 Electrical Setup

- Charge the cell to 100% State of Charge (SOC) using standard CC-CV method

- Measure and record initial open-circuit voltage (OCV)

- Attach thermocouples to the centre surface of the cell

- Enable continuous voltage and temperature data logging

7. Test Conditions (IEC 62660-2)

- Initial SOC: 100%

- Heating Method: Ambient temperature increases in thermal chamber

- Temperature Ramp Rate: 5 °C/min ± 2 °C/min

- Target Temperature: 130 °C

- Soak Duration: 30 minutes at target temperature

- Ambient Pressure: Atmospheric

8. Test Procedure

Step 1: Pre-Test Preparation

- Verify correct cell identification and SOC

- Confirm thermocouple placement and data acquisition readiness

- Ensure chamber door is securely closed

Step 2: Temperature Ramp

- Start heating at the specified ramp rate

- Continuously record:

  - Cell surface temperature

  - Chamber temperature

  - Cell voltage

Step 3: High-Temperature Soak

- Maintain the chamber at 130 °C for 30 minutes

- Observe the cell through monitoring systems for:

  - Swelling

  - Venting

  - Smoke

  - Fire or explosion

Step 4: Cooling Phase

- After completion of soak, turn off heating

- Allow the cell to cool naturally inside the chamber

- Do not remove the cell until temperature falls below 50 °C

9. Post-Test Observation

- Observe the cell for a minimum of 60 minutes after cooling

- Record maximum temperature and voltage behaviour

- Document any delayed events (venting, ignition, rupture)

- Record final physical condition of the cell

10. Acceptance Criteria

A cell passes the Thermal Abuse Test if:

- No fire or explosion occurs during or after the test

- Venting without flame is acceptable

- No violent rupture or projectile hazard is observed

11. Failure Handling

- Secure and isolate the test area immediately in case of failure

- Record detailed timeline, temperature profile, and failure mode

- Quarantine the tested cell for failure analysis

- Inform safety, quality, and engineering teams

12. Documentation & Records

- Temperature vs time data

- Voltage vs time data

- Test setup photographs and video recordings

- Event timeline and observations

- Final test report with PASS / FAIL conclusion